SECTION 05070

BOLTED FASTENERS

PART 1 - GENERAL

1-01	SCOPE:

A.	The Work of this Section consists of furnishing all labor, materials and equipment necessary for installation of bolted fasteners as shown on the drawings.

1-02	STANDARD REFERENCES:

A.	The following standard specifications shall apply to the Work of this Section as indicated:

1.	American Society of Testing Materials (ASTM).

2.	American National Standards Institute (ANSI).

3.	American Institute of Steel Construction (AISC).

PART 2 - MATERIALS

2-01	HIGH STRENGTH BOLTS:

A.	High strength bolts shall conform to the requirements of ASTM A325, High Strength Bolts for Structural Steel Joints.  The bolt dimension shall conform to the current requirements of ANSI B18.2.1 for heavy hex structural bolts.

2-02	ALLOY STEEL BOLTS:

A.	Alloy steel bolts shall conform to the requirements of ASTM A490, Quenched and Tempered Alloy Steel Bolts.

2-03	STANDARD THREADED FASTENERS:

- Standard threaded fasteners shall be stainless type 304 steel square bolts conforming to ASTM A307.

- Heavy loaded fasteners shall be Hilti type HAS-R stainless conforming to ASTM F593 (3/8” to 1”); and, ASTM A193 (1-1/8” to1-1/4”)

2-04	NUTS:

- Stainless 304 Steel Nuts shall conform to ASTM A563, Standard Specification for Carbon and Alloy Steel Nuts. The nut dimension shall conform to ANSI B18.2.2 for heavy hex nuts.

2-05	WASHERS:

A.	Flat, 304 stainless steel circular and square washers shall conform to ASTM F436, Standard Specification for Hardened Steel Washers.

PART 3 - EXECUTION

3-01	INSTALLATION:

A.	Fasteners shall be tightened in properly aligned holes to provide, when all fasteners in the joint are tight, at least the minimum tension required by AISC Specification for Bolted Connections.  The turn-of-the-nut method shall be utilized for all high-strength bolts as defined by AISC Specification for Bolted Fasteners.  The A325 fasteners shall be installed without hardened washers.  A490 shall have a washer both under the nut and the bolt head.

3-02	REUSE:

A.	A490 bolts and galvanized A325 bolts shall not be reused.  Other A325 bolts may be reused, if approved by the Engineer.

3-03	BOLTED PARTS:

A.	The slope of the bolted parts in contact with the bolt head and nut shall not exceed 1:20 with respect to a plane normal to the bolt axis.  Holes shall be punched and reamed, or drilled, and shall have a diameter nominally 1/16-inch in excess of the nominal bolt diameter. Over-size, short slotted and long slotted holes shall conform to the requirements of AISC Specifications for Structural Joints.

3-04	GALVANIZING:

A.	The galvanizing of the bolts, nuts and washers shall conform to the requirements of ASTM A153.

PART 4- MEASUREMENT AND PAYMENT

4-01	MEASUREMENT AND PAYMENT

There will be no direct measurement for installation of bolted fasteners. Payment for this work shall be included as an indirect cost to the associated bid items where bolt installation work is performed.

***END OF SECTION***